PART 1 GENERAL

1.01 SCOPE

A. 	Provide factory fabricated elastomeric expansion waterproofing joint, to prevent the penetration of water at control, expansion or building joints as indicated on architects/engineers drawings, in new or retrofit installations.

1.02 SUBMITTALS

A.	Submit to joint manufacturer drawings indicating location of joint and configurations.

B. 	Manufacturer’s printed literature and installation instructions.

PART 2 PRODUCT

2.01 DESCRIPTION

A. 	Provide flat, vulcanized waterproofing joint integral with the waterproofing membrane to accommodate movements up to: ± 1" [ ± 25 mm] / ± 2" [ ± 50 mm] / ± 10" [± 250 mm] capable of 500% elongation at - 40 °F [- 40 °C] across its length and at all vulcanized points.

B.	All details and connections are factory fabricated by means of vulcanization.

C.	Joint material is to be FlamLINE [20], [40], [240] as supplied by SITURA INC., (888) 474-8872.

.

PART 3 EXECUTION

3.01 INSTALLATION

A. 	Install all components of the system in accordance with the manufacturer’s most recent printed instructions.

B.	The FlamLINE can be used with Self-Adhered Membranes. Each side of the FlamLINE must be primed with a compatible asphalt primer. Once primed the primer must be allowed to flash off.

C.	Encapsulate the FlamLINE material by applying the Self Adhered Membrane to the primed surfaces. Do not apply the Self Adhered Membrane over the gland of the FlamLINE material. The FlamLINE must be completely stripped in. The FlamLINE joint shall not obstruct water flow across its surface and forms a continuous monolithic waterproof barrier. If necessary flat head fasteners can be used. Fastened at 8” [200 mm] on center staggered.

D.	A protection board can be applied over the FlamLINE joint to protect it from mechanical damage. The protection board can be secured to one side of the joint.

E.	Consult the manufacturer for specific application procedures.

END OF SECTION