PART 1 GENERAL

1.01 SCOPE

A. 	Provide factory fabricated elastomeric expansion waterproofing joint, to prevent the penetration of water at control, expansion or building joints as indicated on architects/engineers drawings, in new or retrofit installations.

1.02 SUBMITTALS

A.	Submit to joint manufacturer drawings indicating location of joint and configuration.

B. 	Manufacturer’s printed literature and installation instructions.

PART 2 PRODUCT

2.01 DESCRIPTION

A. 	Provide flat, vulcanized waterproofing joint integral with the waterproofing membrane to accommodate movements up to: ± 1" [ ± 25 mm] / ± 2" [ ± 50 mm] / ± 10" [± 240 mm] capable of 500% elongation at - 40 °F [- 40 °C] across its length and at all vulcanized points.

B.	All details and connections are factory fabricated by means of vulcanization.

C.	Joint material is to be RedLINE [20], [20G], [40], [40G], [240] as supplied by SITURA INC., 1-888-474-8872.

PART 3 EXECUTION

3.01 INSTALLATION

A. 	Install all components of the system in accordance with the manufacturer’s most recent printed instructions.

B.	Apply the first coat of Hot Rubberized Asphalt at the manufacturer’s recommended minimum thickness, embed a reinforcing fabric mesh and apply a second coat of hot asphalt over it. Immediately, embed the RedLINE waterproof expansion joint material, in the hot asphalt, making sure that the bottom polyester fleece is in full contact with the hot asphalt.

C.	Spread an even coat of Hot Rubberized Asphalt on the top surface of the RedLINE expansion joint ensuring the top white polyester fleece is completely covered; embed a reinforcing fabric mesh. Apply a second coat of Hot Rubberized Asphalt on top of the reinforcing fabric mesh at the manufacturer’s minimum recommended thickness. The joint shall not obstruct water flow across its surface and forms a continuous monolithic waterproof barrier.

3.02 PRECAUTIONS

A.	The center of the RedLINE waterproof expansion joint material must be aligned with the center line of the expansion joint gap. Always lay the RedLINE expansion joint material only in lengths of 10 feet [3 m] or less to allow for contact with hot asphalt material. Do not lay the RedLINE in cold asphalt.

3.03 PROTECTION

A.	The joint can be protected by means of a protection board as per manufacturer’s instructions.

END OF SECTION